Brass-Plating a Penny

Brass is a common alloy, used in making many things from housekeys to doorknobs.  You will plate a copper penny with zinc and then melt it into the copper, creating a brass coating.

Materials:

3 pennies, new if possible

250 mL beaker

beaker tongs

crucible tongs or forceps

watch glass

about 2-2.5 g (or more) of granulated zinc or zinc foil

about 25 mL of 1 M ZnCl2

Bunsen burner

Hot plate

Procedures:

- If needed, clean the pennies by using steel wool or vinegar/salt mixture.  Put one penny aside as a control.

- Put the zinc into the beaker and pour the ZnCl2 into the beaker.  Put 2 pennies into the beaker on top of the zinc.  Put the watch glass on top of the beaker.

- Gently heat the solution until it just starts to bubble; do not let it boil or dry out.

- Heat them for several minutes (5 is more than enough)

- Use the tongs or forceps to remove the 2 pennies.  Rinse them in water.  Put one of the pennies aside.

- Take the other silvery penny and move it slowly and horizontally over the flame until you observe it change.  It will be “golden” in color.